PARNISARI ARMS  S.R.L.

# Via Opifici N. 2 - 28040  Lesa ( Novara ) Italia

# Tel. 0322 772152 - Fax 0322 772152Cell.  347 4247858

Partita  Iva / C.F/N. iscrizione registro imprese Novara. 01918100031

E Mail  arms@parnisariarms.com

www.parnisariarms.com

# Mod. RT1OO6

# Anti-Riot Helmet

The anti-riot helmet used by Italian Police, Guardia di Finanza, Agenti di Custodia (Prison Police) and other Law Enforcement throughout the world.

- High impact resistant polycarbonate shell with head ventilation system

- Polystirene inner liner for maximum shock absorbtion

- Padded inner cover made of fire retardant fabric

- 4 mm polycarbonate face shield with up or down locking system

- Moulded neck protector with polycarbonate inserts and fire retardant fabric cover

- Quick release retention system with removable chin protector

- Sizes: 52-62

- Weight: 1.350 grams

- Colours: White, Blue, Light Blue, Green (other available on request)

# Developed and manufactured according with C. T. 38/M  (Italian Police Specs.).

# Technical Specs.

PARNISARI  riot helmet models RTIOO6 is tested under the following specifications:

Shock absorbtion:UNI 7417-75- The helmet, on a headform, is impacted with a 5 kg. mass from an height of 2.5 meters. Transmitted energy must be less than: 15 KNewton	 ECE-ONU n. 22 - 7.3

Penetration (shell):UNI 7417-75-3 kg. Punch from 2 meter.

Penetration (visor):Aluminium projectile (254 grams) at 2 bar air pressure ECE –ONU n. 22 – 7.8

Rigidjty:UNI 7154.4 - 630 N for a time of 5 min.

Fire resistance:UNI 7154 7.7. - Bunsen burner at a distance of 2 cm. from helmet shell

Retention system resistance:UNI 7417-75- Preload 15 kg., dynamic load 10 kg. from 750 mm. ECE-ONU n. 22 - 7.6

Chemical resistance:25 ml. Of gasoline and most commons acid and base solutions (80%  conc.) on shell and face shield for a time of 3 min.

Tests made at ambient (25°C), high (+500) and low (-200C) temperatures with a minimum conditioning time of 4 hours.

# Text boxes

CODICE  NATO

AEA 08